## Slide 1: Defect-Aware ML for Predicting Tensile Strength of E-Glass/Epoxy Composites
SIMULATION-BASED PROTOTYPE
Student | Register number
Jishnu Narayanan | RA2411026010650
Edson Thomas | RA2411026010634
Department of CINTEL
SRM INSTITUTE OF SCIENCE AND TECHNOLOGY
Notes: Sources: project implementation and evaluation metadata; reference numbers match the full project report. Detailed speaker notes are supplied as a separate Word document.

## Slide 2: Introduction and application
Unidirectional E-glass fibres reinforce epoxy and carry load mainly along the fibre direction.
Tensile strength is the maximum tensile stress before failure. 1 MPa = 1 N/mm².
We explore how fibre fraction, voids and fibre/load angle affect an assumed nominal response.
Application: educational scenario comparison, sensitivity studies and regression evaluation.
Scope: a simulator-surrogate prototype. Material qualification and structural design require independent evidence.
Notes: Sources: project implementation and evaluation metadata; reference numbers match the full project report. Detailed speaker notes are supplied as a separate Word document.

## Slide 3: Problem identification research gap and objectives
Problem: the supplied papers do not give a complete compatible three-input tensile dataset. Missing void fractions cannot be replaced with zero.
Project gap: a transparent local workflow that keeps simulated training and literature evidence separate.
Objectives: implement explicit physics, generate reproducible data, compare two regressors and demonstrate checked predictions.
Assess a random holdout and a separate fibre-fraction region shift.
The contribution is an educational implementation. Scientific novelty and real-laminate accuracy remain unestablished.
Notes: Sources: project implementation and evaluation metadata; reference numbers match the full project report. Detailed speaker notes are supplied as a separate Word document.

## Slide 4: Literature review and main findings
35 selected sources: 30 research/data articles and five reviews. 32 are from 2020 onward.
Architecture and direction: Turaka (2024) [1] and Siddgonde (2024) [5] require separate UD and woven interpretations.
Void effects: Ayanoglu (2023) [3] and Hanafiah (2024) [7] show why conditioning, property and void morphology matter.
Surrogates: Mendikute (2023) [11] and Li (2022) [16] motivate simulation-based learning within a defined scope.
Finding: compatible inputs, target property and independent validation matter more than a high isolated score. Full 35-paper matrix and IEEE bibliography are in the report.
Notes: Sources: project implementation and evaluation metadata; reference numbers match the full project report. Detailed speaker notes are supplied as a separate Word document.

## Slide 5: Materials and methods input features
Feature | Unit | Supported range
Fibre volume fraction | % | 20–65
Void content | % | 0–8
Fibre/load angle | degrees | 0–45
At 45% fibres and 2% voids, the physical volume balance leaves 53% matrix.
The saved Random Forest uses these three features only. Volume percentage differs from weight percentage.
Notes: Sources: project implementation and evaluation metadata; reference numbers match the full project report. Detailed speaker notes are supplied as a separate Word document.

## Slide 6: Additional material inputs and nominal defaults
Property | Default | Role
Fibre strength and modulus | 1750 MPa and 73 GPa | Fibre contribution and failure strain
Matrix strength and modulus | 55 MPa and 2.4 GPa | Capped matrix contribution
Transverse and shear strength | 40 MPa and 60 MPa | Off-axis resistance
Physics Explained allows these six properties to vary for a direct simulator calculation.
The saved three-feature forest retains its original nominal parameter snapshot. Changing material controls does not update that forest.
Notes: Sources: project implementation and evaluation metadata; reference numbers match the full project report. Detailed speaker notes are supplied as a separate Word document.

## Slide 7: Methodology
Literature review and UD scope
Separate literature path
Extraction and human review
Comparison only, eligible n = 0
Nominal simulator and three sampled inputs
Generate and validate 2,000 SIMULATED rows
Seed 42 and 5% assumed scatter
Random holdout
1,600 train / 400 holdout
Fit Linear Regression and Random Forest
Separate fibre-region test
1,535 train / 465 test
Fit fresh Linear Regression and Random Forest
Report MAE, RMSE and R² for both splits
Save random-holdout-selected model and demonstrate
Notes: Sources: project implementation and evaluation metadata; reference numbers match the full project report. Detailed speaker notes are supplied as a separate Word document.

## Slide 8: Physics model strength calculation
Matrix stress at fibre failure: sigma_m* = min(sigma_m, E_m sigma_f / E_f)
Longitudinal mixture: X0 = eta Vf sigma_f + (1 - Vf) sigma_m*
Void reductions: Xv = X0 exp(-kf Vv), Yv = Y0 exp(-km Vv), Sv = S0 exp(-km Vv)
Use Vf as a fraction in the mixture. Use Vv in percentage points with kf = 0.010 and km = 0.040 per percentage point.
eta = 1 through 55% fibre, then decreases linearly to 0.80 at 70%. The deployed domain ends at 65%.
The (1 - Vf) term is a simplified matrix contribution with a separate void reduction, not an explicit three-phase volume-resolved model.
Notes: Sources: project implementation and evaluation metadata; reference numbers match the full project report. Detailed speaker notes are supplied as a separate Word document.

## Slide 9: Off-axis model and simulated targets
1 / sigma² = cos⁴(theta) / Xv² + (1 / Sv² - 1 / Xv²) sin²(theta) cos²(theta) + sin⁴(theta) / Yv²
This off-axis Tsai–Hill form combines longitudinal, transverse and shear resistance.
At 0 degrees, sigma = Xv. The analytical 90-degree limit gives Yv, while the app accepts only 0–45 degrees.
Dataset target = nominal sigma × (1 + epsilon), epsilon ~ Normal(0, 0.05²).
The 5% scatter is an assumed data-generation choice. Direct simulator calculations are deterministic.
Notes: Sources: project implementation and evaluation metadata; reference numbers match the full project report. Detailed speaker notes are supplied as a separate Word document.

## Slide 10: Regression models and selection
Linear Regression: a linear combination of the three features plus an intercept. It provides a simple baseline.
Random Forest: average prediction from 120 decision trees, minimum two samples per leaf, random_state 42.
Both candidates use the same 1600/400 random partition.
Select the lower holdout RMSE and save the estimator with feature schema, parameters and provenance.
The saved forest retains its 1600-row fit. It is not refitted on all 2000 rows after selection.
Notes: Sources: project implementation and evaluation metadata; reference numbers match the full project report. Detailed speaker notes are supplied as a separate Word document.

## Slide 11: Evaluation design and metrics
Random holdout: 1600 training rows and 400 selection-holdout rows from the same simulated domain.
Fibre-region experiment: train on 1535 rows with Vf < 55%, test on 465 with Vf ≥ 55%.
MAE: average absolute error in MPa.
RMSE: square root of average squared error in MPa, giving larger deviations more weight.
R²: 1 - residual sum of squares / total target sum of squares. R² is not percentage accuracy.
The region experiment tests one defined shift within the simulator domain, not a different material or all forms of extrapolation.
Notes: Sources: project implementation and evaluation metadata; reference numbers match the full project report. Detailed speaker notes are supplied as a separate Word document.

## Slide 12: Results and discussion
Split and model | MAE MPa | RMSE MPa | R²
Random holdout: Linear Regression | 74.18 | 102.03 | 0.6836
Random holdout: Random Forest | 10.79 | 18.21 | 0.9899
Fibre-region: Linear Regression | 90.99 | 132.68 | 0.6204
Fibre-region: Random Forest | 14.18 | 28.63 | 0.9823
The forest has lower error on both tests. Its higher region-test RMSE indicates reduced reliability in the withheld fibre range.
All metrics compare predictions with noisy simulated targets. Experimental accuracy remains untested.
Notes: Sources: project implementation and evaluation metadata; reference numbers match the full project report. Detailed speaker notes are supplied as a separate Word document.

## Slide 13: Model behaviour under angle changes
Chart: Fibre/load angle (degrees)
| 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26 | 27 | 28 | 29 | 30 | 31 | 32 | 33 | 34 | 35 | 36 | 37 | 38 | 39 | 40 | 41 | 42 | 43 | 44 | 45
Noise-free nominal simulator | 801.5575 | 777.4777 | 716.4115 | 640.2385 | 565.2678 | 498.7048 | 442.11 | 394.6967 | 355.0233 | 321.6576 | 293.3786 | 269.2026 | 248.3537 | 230.224 | 214.3357 | 200.3117 | 187.8519 | 176.7154 | 166.7075 | 157.6692 | 149.4696 | 142.0005 | 135.1713 | 128.9057 | 123.1394 | 117.8173 | 112.8925 | 108.3241 | 104.0772 | 100.121 | 96.4287 | 92.9768 | 89.7444 | 86.7132 | 83.8667 | 81.1904 | 78.671 | 76.2968 | 74.0573 | 71.9428 | 69.9447 | 68.055 | 66.2666 | 64.5729 | 62.968 | 61.4463
Random Forest surrogate | 756.0729 | 755.2137 | 714.5365 | 643.4445 | 572.5728 | 481.1972 | 444.4728 | 419.9721 | 356.9238 | 316.4132 | 291.4967 | 265.612 | 229.1632 | 226.6272 | 217.125 | 193.2228 | 184.6876 | 179.8034 | 170.1861 | 156.0629 | 148.6802 | 142.7603 | 141.147 | 129.8332 | 123.948 | 116.7919 | 117.4549 | 111.3234 | 103.1833 | 101.3927 | 99.7817 | 92.4906 | 87.8198 | 88.7248 | 83.4756 | 79.7326 | 78.4904 | 74.574 | 74.7302 | 73.1445 | 68.9838 | 68.7701 | 66.5337 | 64.7444 | 61.2377 | 60.8691
Fibre fraction 45%, voids 2%. The curves describe the nominal simulator and its fitted surrogate. Independent experimental validity remains untested.
Notes: Sources: project implementation and evaluation metadata; reference numbers match the full project report. Detailed speaker notes are supplied as a separate Word document.

## Slide 14: Software architecture and input checks
Saved model prediction
Three inputs
Vf, voids, angle
Unit and
domain checks
Saved forest
and metadata
Labelled estimate
Scenarios and sensitivity
Separate direct simulator experiment
Three geometry inputs
Six material properties
Nominal equations
and parameter checks
Direct simulator result
No saved-model update
Nine dashboard tabs. 21 recorded software tests passed. Independent experimental validation remains outstanding.
Notes: Sources: project implementation and evaluation metadata; reference numbers match the full project report. Detailed speaker notes are supplied as a separate Word document.

## Slide 15: Demonstration cases and expected outputs
Case | Vf % | Voids % | Angle deg | RF MPa | Direct MPa
Baseline | 45 | 2 | 5 | 481.20 | 498.70
More voids | 45 | 6 | 5 | 457.37 | 443.23
Larger angle | 45 | 2 | 20 | 148.68 | 149.47
Show the SIMULATED label, run the baseline, then change one feature at a time.
Finally show domain rejection and a six-property direct simulator calculation.
RF output is a surrogate-model estimate of the simulator. Direct values also come from assumed equations.
Notes: Sources: project implementation and evaluation metadata; reference numbers match the full project report. Detailed speaker notes are supplied as a separate Word document.

## Slide 16: Literature comparison and validation plan
Four supplied PDFs audited. Eight printed mean-strength rows transcribed from Gopalakrishnan (2016) [28].
All eight remain reviewed = no and lack matched void content. Some also fall outside the supported angle or architecture.
Eligible reviewed comparison rows: n = 0. No experimental-comparison error is reported.
Next: obtain complete matched UD E-glass/epoxy inputs, review each extraction and record test conditions.
Calibrate on designated data, then evaluate separate independent studies with sample counts and MPa errors.
Notes: Sources: project implementation and evaluation metadata; reference numbers match the full project report. Detailed speaker notes are supplied as a separate Word document.

## Slide 17: Conclusion limitations and future enhancement
Delivered: explicit simulator, 2000 labelled samples, two-model comparison, saved forest and working dashboard.
Finding: the forest approximates this configured simulator better than the linear baseline under both splits.
Limits: nominal parameters, one uniform angle, scalar void content, assumed scatter and no independent experimental validation.
Future inputs may include cure conditions, moisture, fibre length, layup and void morphology after obtaining supported relationships or matched data.
Adding interface fields alone cannot make the current three-feature forest use new variables.
Notes: Sources: project implementation and evaluation metadata; reference numbers match the full project report. Detailed speaker notes are supplied as a separate Word document.

## Slide 18: Publication and work in progress
Completed: simulation workflow, trained model, evaluation, dashboard, documentation and software checks.
Available for review: source code, parameter file, model metadata, report and separate speaking guide.
In progress: human review of literature extracts and collection of complete compatible measurement rows.
Next research stage: calibration on separate evidence and evaluation on independent studies.
No research paper has been submitted or published as an outcome of this project.
Notes: Sources: project implementation and evaluation metadata; reference numbers match the full project report. Detailed speaker notes are supplied as a separate Word document.

## Slide 19: Selected references
[1] S. Turaka, R. Chintalapudi, N. Kannaiyan Geetha, B. Pappula, S. Makgato, “Experimental and numerical analysis of the Microstructure and mechanical properties of unidirectional glass fiber reinforced epoxy composites”, Composite Structures, vol. 331, Art. no. 117887, 2024, doi: 10.1016/j.compstruct.2024.117887.
[3] M. O. Ayanoglu, L. A. Carlsson, E. Du, “Effects of void content on the moisture uptake and mechanical strength of a glass/epoxy composite”, Journal of Composite Materials, vol. 57, no. 2, pp. 325-336, 2023, doi: 10.1177/00219983221144500.
[5] N. Siddgonde, V. Kaushik, A. Ghosh, “Experimental and numerical characterization of E-glass/epoxy plain woven fabric composites containing void defects”, Aerospace Science and Technology, vol. 155, Art. no. 109731, 2024, doi: 10.1016/j.ast.2024.109731.
[7] Nur Hafzareen Md Hanafiah, Abdul Rahim Othman, Mark Ovinis, “Significant Effect of Vacuum Bagging Processing on Inter-Laminar Shear Strength and Voids of Composite in Oven Cure”, Journal of Advanced Research in Applied Sciences and Engineering Technology, vol. 37, no. 1, pp. 69-81, 2024, doi: 10.37934/araset.37.1.6981.
[11] J. Mendikute, M. Baskaran, I. Llavori, E. Zugasti, L. Aretxabaleta, J. Aurrekoetxea, “Predicting the effect of voids generated during RTM on the low-velocity impact behaviour by machine learning-based surrogate models”, Composites Part B: Engineering, vol. 260, Art. no. 110790, 2023, doi: 10.1016/j.compositesb.2023.110790.
Full 35-source IEEE bibliography and review matrix: project report Chapter 2 and References. Numbering matches that report.
Notes: Sources: project implementation and evaluation metadata; reference numbers match the full project report. Detailed speaker notes are supplied as a separate Word document.

## Slide 20: Selected references and full bibliography
[16] M. Li, H. Zhang, S. Li, W. Zhu, Y. Ke, “Machine learning and materials informatics approaches for predicting transverse mechanical properties of unidirectional CFRP composites with microvoids”, Materials & Design, vol. 224, Art. no. 111340, 2022, doi: 10.1016/j.matdes.2022.111340.
[20] A. Alsheghri, A. Alhammadi, V. Drakonakis, H. Doumanidis, I. Barsoum, M. Maalouf, “Predicting mechanical properties of CFRP composites using data-driven models with comparative analysis”, PLOS ONE, vol. 20, no. 4, pp. e0319787, 2025, doi: 10.1371/journal.pone.0319787.
[24] K. Zhou, H. Sun, R. Enos, D. Zhang, J. Tang, “Harnessing deep learning for physics-informed prediction of composite strength with microstructural uncertainties”, Computational Materials Science, vol. 197, Art. no. 110663, 2021, doi: 10.1016/j.commatsci.2021.110663.
[25] M. Mehdikhani, C. Breite, Y. Swolfs, M. Wevers, S. V. Lomov, L. Gorbatikh, “A dataset of micro-scale tomograms of unidirectional glass fiber/epoxy and carbon fiber/epoxy composites acquired via synchrotron computed tomography during in-situ tensile loading”, Data in Brief, vol. 34, Art. no. 106672, 2021, doi: 10.1016/j.dib.2020.106672.
[28] M. Gopalakrishnan, S. Muthu, R. Subramanian, R. Santhanakrishnan, L. Karthigeyan, “Tensile Properties Study of E-Glass/Epoxy Laminate and π/4 Quasi-Isotropic E-Glass/Epoxy Laminate”, Polymers and Polymer Composites, vol. 24, no. 6, pp. 429-446, 2016, doi: 10.1177/096739111602400606.
Full 35-source IEEE bibliography and review matrix: project report Chapter 2 and References. Numbering matches that report.
Notes: Sources: project implementation and evaluation metadata; reference numbers match the full project report. Detailed speaker notes are supplied as a separate Word document.